Supporting Information

Cheminformatics and Machine Learning for Quasi-2D Perovskites: Emission Energy Prediction and the Limits of EQE Modelling

Table S1. Dataset Statistics of file: data/SF_DATA_EMISSION_PEAK.xlsx, sheet SF_DATA_EMISSION_PEAK_NEW.

| Statistic | Value |
| --- | --- |
| Records (N) | 283 |
| Training | 226 (80%) |
| Testing | 57 (20%) |
| Stratification key | IS_MIXED_SPACERS_SPACER (> 0 vs. 0) |
| Eph (eV) | 1.53 – 3.06 |
| λ (nm) | 405 – 810 |
| Mixed-spacer count | 46 (16.3%) |
| Unique primary IUPAC | 22 |

Table S2. Wavelength bin distribution.

| Wavelength Range | Label | Number of records | Fraction |
| --- | --- | --- | --- |
| 400 – 480 | Violet/blue | 35 | 12.4% |
| 480 – 550 | Green / yellow | 195 | 69.0% |
| 550 – 650 | Orange / red | 6 | 2.1% |
| 650 – 900 | Deep red / NIR | 47 | 16.6% |

Table S3. Matrix dimensions.

| Stage | Shape | Notebook output |
| --- | --- | --- |
| Raw Excel | 283 × 37 | (283, 37) |
| After AddHs RDKit + OHE | 283 × 462 | (283, 462) |
| Unique SMILES processed | 30 |  |
| After ¦r¦ > 0.90 | 283 × 289 | 173 columns dropped |

Figure S1. RFECV cross-validation RMSE versus number of retained features; vertical marker at 31.

Table S4. Sample-to-feature ratios.

| Feature set | p | Ntrain | N/p |
| --- | --- | --- | --- |
| SelectFromModel (canonical) | 13 | 226 | 17.38 |
| RFECV (canonical) | 31 | 226 | 7.29 |
| RFECV no AddHs (ablation) | 39 | 226 | 5.79 |

Table S5. Thirteen features - select_from_model

| S.No. | Feature Name |
| --- | --- |
| 1 | CL_PRIMARY_ORGANIC_HALIDE |
| 2 | BR_PRIMARY_ORGANIC_HALIDE |
| 3 | SPACER_TO_PB_RATIO |
| 4 | PbCl2 |
| 5 | PbBr2 |
| 6 | CsBr_TO_Pb |
| 7 | CsI_TO_Pb |
| 8 | FABr_TO_Pb |
| 9 | FAI_TO_Pb |
| 10 | SOLVENT_DMF |
| 11 | Pri_VSA_EState4 |
| 12 | Sec_HallKierAlpha |
| 13 | Sec_PEOE_VSA6 |

Training / testing shapes: (226, 13) and (57, 13).

Table S6. Thirty-one features - RFECV.

| S. No. | Feature Name |
| --- | --- |
| 1 | BR_PRIMARY_ORGANIC_HALIDE |
| 2 | PRIMARY_SPACER_FRACTION |
| 3 | SPACER_TO_PB_RATIO |
| 4 | PbCl2 |
| 5 | PbBr2 |
| 6 | CsBr_TO_Pb |
| 7 | CsI_TO_Pb |
| 8 | FABr_TO_Pb |
| 9 | FAI_TO_Pb |
| 10 | SOLVENT_DMF |
| 11 | SOLVENT_DMSO |
| 12 | Pri_qed |
| 13 | Pri_SPS |
| 14 | Pri_BCUT2D_MWHI |
| 15 | Pri_BCUT2D_MWLOW |
| 16 | Pri_BCUT2D_LOGPLOW |
| 17 | Pri_BCUT2D_MRHI |
| 18 | Pri_Kappa3 |
| 19 | Pri_PEOE_VSA10 |
| 20 | Pri_PEOE_VSA7 |
| 21 | Pri_SMR_VSA1 |
| 22 | Pri_VSA_EState4 |
| 23 | Pri_VSA_EState7 |
| 24 | Pri_VSA_EState8 |
| 25 | Pri_NumHeteroatoms |
| 26 | Pri_NumRotatableBonds |
| 27 | Pri_Phi |
| 28 | Sec_BCUT2D_MWHI |
| 29 | Sec_HallKierAlpha |
| 30 | Sec_Kappa3 |
| 31 | Sec_PEOE_VSA6 |

Training / testing shapes: (226, 31) and (57, 31).

Table S7. Emission Photon Energy —SelectFromModel (13 features)+ Hyperparameter-tuned model. Source: add_hydrogens_tuned_select_from_model.ipynb.

| Rank | Model | R² | RMSE (eV) | MAE (eV) |
| --- | --- | --- | --- | --- |
| 1 | SVR (RBF) | 0.952715 | 0.074335 | 0.047942 |
| 2 | Gaussian Process | 0.920381 | 0.096459 | 0.060961 |
| 3 | CatBoost | 0.874856 | 0.120931 | 0.062522 |
| 4 | XGBoost | 0.756337 | 0.168744 | 0.070986 |
| 5 | Random Forest | 0.747938 | 0.171628 | 0.083796 |

Figure S2. Ten-fold cross-validated R², RMSE, and MAE for the champion SVR-RBF model across all 283 samples. Each bar represents one fold. The dashed line indicates the mean and the shaded band represents ±1 standard deviation across folds.

Figure S3. Learning curve for the champion SVR-RBF model evaluating the root-mean-square error (RMSE) as a function of training set size. The solid lines represent the mean RMSE across 10 cross-validation folds, and the shaded regions represent ±1 standard deviation. The convergence and flattening of the cross-validation error (red line) indicates that the model is well-fitted and the dataset size is sufficient for the model to learn the underlying patterns without requiring substantially more data.

Figure S4: SHAP for the select_from_model + Gaussian Process model.

Figure S5: SHAP for the select_from_model + Catboost model.

Figure S6: SHAP for the select_from_model + XGBoost model.

Figure S7: SHAP for the select_from_model + Random Forest model.

Table S8. Emission Photon Energy — RFECV (31 features)+ Hyperparameter-tuned model. Source: add_hydrogens_tuned_rfecv.ipynb.

| Rank | Model | R² | RMSE (eV) | MAE (eV) |
| --- | --- | --- | --- | --- |
| 1 | SVR (RBF) | 0.919559 | 0.096955 | 0.053890 |
| 2 | Gaussian Process | 0.876814 | 0.119981 | 0.072528 |
| 3 | CatBoost | 0.861979 | 0.127001 | 0.066114 |
| 4 | XGBoost | 0.746257 | 0.172199 | 0.072514 |
| 5 | Random Forest | 0.690493 | 0.190182 | 0.086730 |

Figure S8: SHAP for the RFECV + SVR (RBF).

Figure S9: SHAP for the RFECV + Gaussian Process.

Figure S10: SHAP for the RFECV + CatBoost.

Figure S11: SHAP for the RFECV + XGBoost.

Figure S12: SHAP for the RFECV + Random Forest model.

Table S9. Emission Photon Energy — RFECV (31 features) + untuned model. Source: add_hydrogens_baseline_rfecv.ipynb.

| Rank | Model | R² | RMSE (eV) | MAE (eV) |
| --- | --- | --- | --- | --- |
| 1 | Gaussian Process | 0.876814 | 0.119981 | 0.072528 |
| 2 | CatBoost | 0.857190 | 0.129185 | 0.069607 |
| 3 | SVR (RBF) | 0.819187 | 0.145361 | 0.073809 |
| 4 | XGBoost | 0.809737 | 0.149111 | 0.068635 |
| 5 | Random Forest | 0.699186 | 0.187492 | 0.085629 |

Figure S13: SHAP for the RFECV + Gaussian Process model without hyperparameter tuning.

Figure S14: SHAP for the RFECV + CatBoost  model without hyperparameter tuning.

Figure S15: SHAP for the RFECV + SVR (RBF) without hyperparameter tuning.

Figure S16: SHAP for the RFECV + XGBoost without hyperparameter tuning.

Figure S17: SHAP for the RFECV + Random Forest without hyperparameter tuning.

Table S10. Emission Photon Energy - comparison of best SVR models.

| Notebook | Features | Hyperparameter Tuned | SVR R² | SVR RMSE (eV) |
| --- | --- | --- | --- | --- |
| select_from_model + SVR | 13 | Yes | 0.953 | 0.074 |
| RFECV + SVR | 31 | Yes | 0.920 | 0.097 |
| RFECV + SVR | 31 | No | 0.819 | 0.145 |

Table S11. EQE Dataset summary.

| Statistic | Value |
| --- | --- |
| Sheet | EQE_CLEANED |
| Records | 266 |
| EQE range (%) | 0.002 – 30.84 |
| Unique HTL | 34 |
| Unique ETL | 13 |

Table S12. RFE-20 tuned models. Source: eqe_percent/rfe_20_features_tuned.ipynb.

| Model | R² | RMSE (% EQE) | MAE (% EQE) |
| --- | --- | --- | --- |
| Tuned XGBoost | 0.512 | 5.01 | 3.77 |
| Tuned Random Forest | 0.478 | 5.18 | 3.88 |
| Tuned CatBoost | 0.443 | 5.35 | 3.75 |

Table S13. CatBoost model with ETL, HTL and additive categorical fields. Source: eqe_percent/catboost_only.ipynb.

| Metric | Value |
| --- | --- |
| R² | 0.570 |
| RMSE (% EQE) | 4.42 |
| MAE (% EQE) | 3.25 |